Cumulative Machine Learning and Digitalization Insights into Grinding Processes with Multi-Alloy and Multi-Cooling Variability

Abstract

The grinding process is inherently complex and non-homogeneous due to the simultaneous influence of multiple parameters, typically ranging from 8 to 15, which directly affect surface roughness and overall workpiece quality. This complexity is particularly critical in high-precision industries such as aerospace and medical device manufacturing. Despite its industrial relevance, most existing studies have focused on single-alloy implementations, leaving a gap in cumulative approaches that treat alloy type as a variable predictor alongside other process parameters.

This study addresses that gap by consolidating three distinct grinding datasets—Inconel 718, Steel ST34, and Aluminum—under diverse cooling conditions into a single universal dataset. A multi-criteria decision-making (MCDM) framework was introduced to harmonize 16 initial parameters, resulting in a consolidated dataset of 10 key predictors, including alloy type and coolant type as novel variables. Preprocessing and statistical analysis revealed the limitations of conventional methods such as N-Way ANOVA, underscoring the need for advanced machine learning approaches.

Five machine learning models—Support Vector Regression (SVR), Gaussian Process Regression (GPR), Artificial Neural Networks (ANN), Ensemble methods, and k-Nearest Neighbors (KNN)—were implemented with Bayesian hyperparameter tuning. Among them, the Ensemble model achieved the highest predictive accuracy (R2=0.83, mean accuracy = 83% on testing), followed closely by GPR. SHAP-based sensitivity analysis confirmed the dominant influence of specific removal rate, grinding wheel type, and dressing speed, while validating alloy type and coolant type as significant contributors.

Finally, a Green Machining Framework Application was developed, integrating the dataset, models, and sensitivity analysis into a user-friendly platform. This tool enables parameter input, prediction, and interpretability, offering a scalable solution for multi-alloy grinding optimization and advancing sustainable, intelligent manufacturing practices.

# Introduction

The continuing effort to achieve better surface integrity and accuracy of machined components remains a major component of high technology manufacturing particularly of critical applications in the aerospace, energy, and biomedical sectors. Grinding is the finishing operation that deserves most of the attention when it comes to acquiring both a smooth surface and close dimensional tolerance to a wide variety of engineering materials, spanning the common steels to the more advanced superalloys [1, 2]. The appearance of a ground surface, in the first place, roughness (Ra, Rz), is not only an aesthetic characteristic, but also a significant parameter of performance that can influence the fatigue life of the final product, tribological characteristics, corrosiveness, and life cycle [3, 4].

However, this process of grinding is a complex physical and chemical process and is influenced by numerous factors that are not always linear. They are the grinding (wheel speed, workpiece speed, depth of cut, feed rate) specifications, the wheel (abrasive type, grit size, bond material) specifications, the dressing (dressing depth ad, dressing lead sd, dresser type) specifications, and the cooling and lubrication (dry, wet, Minimum Quantity Lubrication - MQL) specifications [5]. Surface roughness is extremely difficult to accurately predict and control as these variables are very complex interacting with each other. More traditional empirical and statistical modeling techniques, such as Response Surface Methodology (RSM) and Analysis of Variance (ANOVA), often fail to describe non-linear relationships, such as qualitative variables like coolant type or dresser geometry [6, 7].

With the emergence of Industry 4.0 and the digitalization of the manufacturing process, it is now possible to bypass these issues through data-driven means. Machine Learning (ML), a subfield of artificial intelligence, is now a convenient method to model complex systems without having to employ explicit physical formulations [8]. It is extremely excellent at forecasting machining results because it is able to gain knowledge of previous information and identify latent trends. Universal function approximators known as Artificial Neural Networks (ANNs) have been popularly used to simulate the grinding processes [9, 10]. Indicatively, Chandrasekaran and Devarasiddappa [11] applied a feedforward ANN to predict the roughness of the surface to be obtained after grinding Al-SiC composites. In [12], Govindhasamy et al. controlled and enhanced an industrial grinding process with ANN models. Along with ANNs, other robust machine learning algorithms such as Gaussian Process Regression (GPR) and Support Vector Regression (SVR) have demonstrated that they are capable of working with high-dimensional and non-linear data particularly well. They are able to provide you with both predictions and confidence intervals of that prediction [13, 14].

In milling, Shang et al. [15] demonstrated that extreme learning machines with sensor-data fusion outperform classical regression when combining cutting parameters and vibration signals. Bai et al.[16] advanced this by integrating mechanistic descriptors with ML surrogates, achieving both predictive accuracy and physical interpretability. Ruan et al. [17] introduced NASPrecision, a neural-architecture-search framework that automatically identifies optimal deep models across multiple datasets, yielding lower MAPE and RMSE than multi-model baselines.

For online monitoring, Shehzad et al. [18] proposed a hybrid CNN-LSTM framework for fly-cutting of copper, using tooltip acceleration signals to surpass conventional CNN or LSTM approaches. Their later work [19] validated a fully information-driven monitoring system, showing industrial-grade feasibility. Sizemore et al. applied supervised classifiers in diamond machining of germanium, effectively distinguishing acceptable from defective surfaces and guiding parameter selection in optical manufacturing. In end-milling, Balonji et al. [20] compared soft-computing techniques for Al6061, achieving high R2and low RMSE values, confirming the robustness of optimized models.

Electric discharge machining (EDM) and wire EDM (WEDM) have also benefited from ML. Abbas et al. [21] used ensemble tree methods (decision trees, random forests, XGBoost) to predict surface roughness in die-sinking EDM of Al-matrix composites, outperforming classical response-surface models. Gurgenc and Altay [22] showed that ensemble and evolutionary neural networks surpass traditional MLPs in WEDM of magnesium alloys, reducing experimental effort.

Grinding studies further illustrate ML’s versatility. Uçar and Katı [23] modeled cylindrical grinding of Al-MMCs with predictive ML frameworks, while Samavatian et al. [24] introduced analytically guided ML for steel grinding, combining domain knowledge with data-driven inference.

Despite such development, a review of the literature reveals that several gaps exist. First, many studies are performed with small datasets or may result into models that are too specialized and do not apply in different scenarios [25]. Second, most crucial process parameters (in particular, dressing conditions (ad, sd) and cooling (such as MQL using various oils or gases) parameters are either not considered at all or assumed to be constant. This renders the model relatively unhelpful in a broad spectrum of industrial applications [26, 27]. Third, a tendency towards focusing on a single alloy leads to a lack of a comprehensive comparative study that would demonstrate machine learning model flexibility across materials with very different mechanical and thermal properties [28].

We have previously addressed these gaps through systematic studies of specific alloys. Forthermore previously studied the effects of dressing parameters and four different cooling conditions (Dry, Wet, MQL-Air, MQL-Argon) on roughness on the surface of steel workpeace using artificial neural networks (ANNs) with various architectures in [7]. In [29], the extended analysis to include the geometry of the dressing tool (single-point vs. four-point diamond dresser) to grind the nickel-based superalloy Inconel 738. In the other study [30] the prediction of the grinding forces along with the surface roughness of UNS S34700 stainless steel, applying a multi-algorithm framework (ANN, GPR, SVR) and including explicitly the qualitative parameters (three types of wheels, four types of coolants). A general overview of existing literature and the gaps which has been addressed in this work has been demonstrated in Table 1.

Table 1. A general framework of existing research employing machine learning techniques in grinding and related machining processes.

| Study Focus (Dataset) | Alloy | Machining Process | Key ML Technologies | Reported Accuracy Metrics |  |
| --- | --- | --- | --- | --- | --- |
| Surface roughness prediction with sensor-data fusion | Optical components (ultra-precision parts) | Ultra-precision milling | Extreme Learning Machine (ELM) with fused cutting + vibration signals | Lower prediction error than classical regression; improved Ra prediction | [15] |
| Hybrid physics–data-driven roughness model | Ultra-precision machined components | Ultra-precision machining (general framework) | Hybrid mechanistic descriptors + ML surrogates (physics-informed ML) | High predictive accuracy; preserves physical interpretability | [16] |
| NASPrecision multi-stage learning framework for Ra prediction | Multiple ultra-precision machining datasets | Ultra-precision machining (multi-dataset) | Neural Architecture Search (NAS) + deep networks, multi-stage learning | Significant reductions in MAPE and RMSE vs conventional single-model baselines | [17] |
| Online surface roughness monitoring in fly-cutting | Copper workpieces | Ultraprecision fly-cutting | Hybrid CNN–LSTM deep network (tooltip acceleration time series) | Superior performance vs standalone CNN or LSTM; robust online Ra monitoring | [18] |
| Surface quality classification in ultra-precision machining | Single-crystal germanium | Ultra-precision diamond machining | Supervised ML classifiers (e.g. tree-based / statistical models) | High classification accuracy; reliable separation of acceptable vs defective surfaces | [19] |
| Surface roughness prediction in CNC end-milling | Al6061 (aluminum alloy) | CNC end-milling | Soft-computing techniques (ANN-type and related models) | High R² and low RMSE for optimized models; effective Ra prediction | [20] |
| Surface integrity and Ra prediction in die-sinking EDM | Al-matrix composites | Die-sinking EDM | Decision Trees, Random Forests, XGBoost | Improved prediction vs response-surface models; better fit to non-linear behaviour | [21] |
| Surface roughness prediction in WEDM of AZ91D | AZ91D magnesium alloy | Wire EDM (WEDM) | MLP, ensemble neural networks, evolving product-unit NN | Ensemble/evolutionary NNs outperform standard MLP; reduced experimental effort | [22] |
| Surface roughness prediction in cylindrical grinding | Al-based metal matrix composite | Cylindrical grinding | ML-based predictive model (ANN / regression-type ML) | High R² and low prediction error for Ra | [23] |
| Analytically guided ML for roughness in steel grinding | Steel (grinding processes) | Grinding (steel) | Analytically guided ML (physics-informed features + ML models) | Improved Ra prediction vs purely empirical models (R², RMSE enhanced) | [24] |
| Surface Roughness Prediction | St37 | Surface Grinding | ANN (MLP) | MSE, R² | [7] |
| Surface Roughness Prediction | Al-SiC MMC | Cylindrical Grinding | ANN (FFNN) | Prediction Accuracy | [11] |
| Process Control & Optimization | Aluminum | Disk Grinding | ANN | N/A (Control Strategy) | [12] |
| Effects of Dressing/Cooling | Inconel 738 | Surface Grinding | - (Experimental) | - | [26] |
| Grinding Params under Cooling | Inconel 751 | Grinding | SVM, Boosted Trees, GPR | R², RMSE | [28] |
| Surface Roughness Prediction | Inconel 738 | Surface Grinding | ANN (Deep MLP) | MSE, R², RMSE, MAE | [29] |
| Roughness & Force Prediction | UNS S34700 | Surface Grinding | ANN, GPR, SVR, GA | R², RMSE, MAPE, Accuracy % | [30] |
| Comparative ML Analysis | Cumulative approach to include St37, Inconel 738, Al6061 Concurrently | Surface Grinding | SVR, GPR, ANN, KNN and Ensemble method | R², RMSE, MAPE, Accuracy % Talyor diagram approach | This Work |

The purpose of this work is to integrate and generalize our research, and to carry out a serious and comparative implementation of optimized machine learning methods in three different alloy systems: UNS34700 steel, Inconel 738 superalloy, and Aluminum 6061. The present work makes use of the extensive data sets made available through our previous experimental activities [29–31].

Based on the limitations arising from previous studies and the generalization approach for implementing machine learning methods in the grinding domain, the following goals will be considered:

- To design and enhance high-fidelity predictive models of surface roughness and grinding forces using a collection of machine learning algorithms.

- In order to do a comparative analysis of the model performance with each of the three alloys, it is important to demonstrate how the properties of the materials influence the accuracy of the predictions.

- To quantify the impact of qualitative factors that are usually given minimal attention, such as the dressing tool and sophisticated cooling strategies, by incorporating them as significant model inputs.

- To develop a powerful framework for selecting the most effective ML methods, consdering the nature of the machining process and material, which will assist in developing smart, data-driven grinding systems.

This study provides a unified model of how machine learning can be applied to different materials, providing valuable insights and viable suggestions for attaining precision grinding in an industrial environment, thus contributing to the realization of fully automated and optimized machining processes.

# Methods and Materials

## Grinding Process Overview

The conventional grinding process begins with selecting an appropriate grinding wheel and preparing it through a dressing procedure, a step that is often overlooked in academic investigations despite its critical role in determining wheel sharpness and cutting efficiency. Once the wheel is dressed, the grinding parameters are adjusted according to the specific workpiece material, and the process is initiated. In many studies, grinding conditions are re‑established in a controlled and homogeneous manner across different materials to ensure comparability. However, in the present work this strategy is deliberately avoided. To develop a universal machine learning framework that is flexible across diverse conditions and materials, the datasets must incorporate variability rather than uniformity. This variability introduces uncertainty into the modeling process, which strengthens the robustness of the predictive algorithms and aligns with the principle of generalizability in machine learning. For this reason, the grinding procedures implemented here are briefly described, while detailed experimental setups are provided in Appendix A.

### Inconel 738 Grinding Experimental Campaign

Grinding experiments on Inconel 738 were conducted using a Prompt 300–1000 machine on specimens of 200 × 40 × 16 mm. Diamond dressing tools with single‑edge and four‑edge configurations were applied at a 10° angle, and an Al₂O₃ wheel operated at a constant cutting speed of 47 m/s with a fixed depth of cut of 10 μm. Prior to each trial, the wheel was subjected to multiple dressing cycles under varying conditions. Cooling strategies included conventional wet machining with water‑miscible coolant and minimum quantity lubrication (MQL) using vegetable oil. Surface roughness was measured under each condition to evaluate the influence of dressing and cooling strategies on machining performance [29].

### UNS S34700 Stainless Steel Experimental Campaign

Further investigations were carried out on hardened stainless steel UNS S34700 using an M7135A surface grinding machine operating in plunge mode. Three grinding wheels of varying abrasive composition were employed to assess performance under different coolant types. The study focused on how variations in wheel composition, coolant type, and depth of cut influenced surface roughness and grinding forces. Both tangential and normal forces were measured, and the results highlighted the direct impact of qualitative and quantitative parameters on grinding behavior [30].

### AA6061 Aluminum Alloy Experimental Campaignc

The grinding behavior of AA6061 aluminum alloy was examined using the same M7135A machine in plunge mode. Tests explored optimal ranges for lubricant application and compressed air flow, employing both synthetic and vegetable oils. Three grinding wheels with different abrasive compositions, grain sizes, and hardness levels were used to capture the influence of wheel characteristics. Cooling strategies included dry compressed air, MQL with vegetable oils of varying viscosities, and conventional water‑based fluid. These conditions were applied across multiple depths of cut to assess their impact on surface integrity and grinding performance, providing a comprehensive view of how wheel properties and cooling methods interact in aluminum grinding [31].

## Cumulation Procedure

Grinding processes are governed by a complex set of parameters—typically ranging from 8 to 15—as outlined in the Köhler study [32]. These parameters span geometrical like ( wheel speed, feed rate, depth of cut) and environmental factors (e.g., coolant type, wheel material), all of which significantly influence final surface roughness. Despite the depth of parameter studies, the inclusion of multiple workpiece materials remains rare. Zhang et al. [33] emphasize this limitation by focusing solely on nickel-based superalloys, while Rodriguez et al. [34] explore interrupted geometries in AISI 4340 steel, considering groove count, feed rate, and flood cooling. Chowdhury et al. (2024) [35] highlight the importance of wheel speed, feed rate, depth of cut, and wheel material in multi-criteria decision-making (MCDM) frameworks, reinforcing the need for integrated parameter selection.

To address this gap, the current study introduces a cumulative decision-making platform that synthesizes grinding parameters from multiple sources, including recent works [29, 30] he platform follows five structured rules to evaluate parameter adjustment across datasets:

- Alloy type is treated as a variable in all datasets to reflect its influence on grinding behavior.

- Each dataset defines its own fixed and variable parameters, preserving experimental integrity.

- If a parameter varies in any dataset, it is treated as variable in the cumulative dataset—even if fixed elsewhere.

- A parameter is considered fixed only if it remains constant across all datasets, ensuring consistency.

- Parameters unique to one study and absent in others are excluded, acknowledging MCDM limitations.

This framework allows the cumulative dataset to grow organically, integrating shared predictors while maintaining flexibility. Surface roughness serves as the observed output, and the cumulative dataset’s value is proportional to the sum of all acceptable datasets. By harmonizing parameter variability across studies, this approach enables adaptive learning and robust prediction, especially in multi-alloy, multi-cooling scenarios where traditional single-material models fall short

## Data-Driven Approach

The transition from empirical, trial-and-error methods to data-driven modeling represents a fundamental paradigm shift in grinding process optimization. Traditional approaches often rely on isolated experiments with narrow parameter scopes, making them inadequate for capturing the nonlinear, multi-variable nature of grinding—especially when alloy type, cooling strategy, and geometric conditions vary across industrial applications. In contrast, data-driven methodologies enable the systematic integration of diverse datasets, allowing predictive models to learn from historical patterns and generalize across unseen combinations. This shift is particularly critical in high-precision domains such as aerospace and medical manufacturing, where surface roughness must be tightly controlled despite fluctuating process conditions [29, 30, 33, 36, 37].

While the efficacy of data-driven approaches in grinding is increasingly evident, a critical limitation persists across the cited studies: the alloy type remains constant within each experimental framework, constraining the generalizability of their models. This homogeneity, though methodologically convenient, restricts the scope of predictive learning in environments where material variability is intrinsic to production. Nevertheless, the sophistication of the machine learning architectures employed—ranging from neural networks enhanced by genetic and particle swarm optimization of GH4169 [36], to layered signal acquisition systems for 40Cr steel [37], and stochastic abrasive modeling for GH404 [33] demonstrates the field’s readiness to transcend traditional boundaries . These models are not merely statistical tools; they function as adaptive interpreters of complex, nonlinear interactions between grinding parameters and surface morphology. The application of support vector regression and artificial neural networks to Ti-6Al-4V further exemplifies this shift, revealing latent interdependencies that elude conventional regression [29]. Collectively, these studies underscore the necessity of a cumulative, alloy-inclusive framework the one capable of integrating heterogeneous datasets and dynamically adjusting to variable input conditions. Such a framework would not only enhance predictive fidelity but also enable real-time decision-making in multi-material grinding scenarios, where parameter interactions are both alloy-specific and context-dependent.

While these studies validate the effectiveness of data-driven techniques, they often focus on a single alloy type, limiting their generalizability. The current research addresses this gap by proposing a cumulative framework that incorporates multiple alloys and cooling strategies as variable parameters. This enables adaptive learning across heterogeneous datasets and supports continuous improvement as new data is added. By leveraging machine learning models capable of capturing nonlinear relationships, the grinding process evolves from a static, rule-based operation into a dynamic, intelligent system—one that responds to variability with precision and insight.

## Machine Learning Models

### SVR

Support Vector Regression (SVR) is a powerful kernel-based supervised learning algorithm tailored for predicting continuous outcomes [38, 39]. It constructs a regression function that approximates target values within a specified tolerance margin ε, while simultaneously minimizing model complexity. Unlike conventional regression techniques that often overfit or underperform in nonlinear domains, SVR prioritizes generalization by allowing controlled deviations from the true outputs. This balance between precision and flexibility makes SVR particularly well-suited for modeling surface roughness in grinding processes, where intricate, nonlinear interactions among parameters—such as wheel speed, feed rate, coolant type, and alloy type—govern the final outcome [40].Once trained, SVR expresses its prediction function using the kernel trick:

| f(x)=i=1n(αi-αi*)K(xi,x)+b | (1) |
| --- | --- |

Where αi,αi*are Lagrange multipliers derived during optimization, K(xi,x)is the kernel function (linear, polynomial, Gaussian) and bis the bias term.

This formulation enables SVR to operate efficiently in high-dimensional feature spaces without explicitly computing the nonlinear transformation. By leveraging kernel-based mappings, SVR captures complex relationships between grinding parameters and surface characteristics, making it an indispensable tool for predictive modeling in multi-variable, alloy-sensitive environments.

### GPR

Gaussian Process Regression (GPR) is a nonparametric, Bayesian approach to regression that models distributions over functions rather than estimating fixed parameters. Unlike traditional regression models that yield point estimates, GPR provides both predictions and uncertainty bounds, making it especially valuable in domains where data is sparse, noisy, or nonlinear. It assumes that any finite set of function values follows a joint Gaussian distribution, governed by a mean function and a covariance kernel that encodes similarity between input points [41, 42].

This probabilistic framework enables GPR to adapt flexibly to complex data structures without requiring explicit functional forms [43]. It is particularly effective in high-dimensional spaces, where relationships between variables are intricate and traditional parametric models may fail to generalize.

In the process of GPR the predictive distrbution function define by

| f(x*)∣X,y,x*∼N(μ(x*),σ2(x*)) | (2) |
| --- | --- |

with:

| μ(x*)=k(x*,X)[K(X,X)+σn2I]-1y σ2(x*)=k(x*,x*)-k(x*,X)[K(X,X)+σn2I]-1k(X,x*) | (3) |
| --- | --- |

Here K(X,X)is the covariance matrix of training inputs, σn2is the noise variance, Iis the identity matrix.

This formulation enables GPR to deliver both predictions and confidence intervals, making it ideal for adaptive control and robust modeling in grinding systems.

### Ensemble

Ensemble regression is a predictive modeling strategy that combines multiple base learners to produce a more accurate and robust output than any individual model alone. The central idea is that diverse models trained on different data subsets or architectures can capture complementary aspects of the input-output relationship. As emphasized by [44] this aggregation reduces variance and improves generalization, especially in noisy or nonlinear regression tasks. The ensemble prediction is typically computed as a weighted sum of individual model outputs

| y=i=1Rwifi(x) | (4) |
| --- | --- |

where Ris the number of base regressors, fi(x)is the prediction from the ithmodel, and wiis its assigned weight.

One common ensemble strategy is bagging (Bootstrap Aggregating), which trains each model on a randomly sampled subset of the data. This introduces diversity and stabilizes predictions. Another is boosting, where models are trained sequentially, each correcting the errors of its predecessor. Boosting often uses adaptive weights based on model performance, leading to the formulation

| y=i=1Tαtht(x) | (5) |
| --- | --- |

where ht(x)is the weak learner at iteration t, and αtis its weight. Notes by [45, 46] highlight how boosting reduces bias while bagging reduces variance—both contributing to ensemble strength. [44] further extend this concept to deep learning, proposing ensembles of neural networks trained independently and fused via weighted averaging or meta-learners.

The effectiveness of ensemble regression depends on the diversity and independence of its components. When base models make uncorrelated errors, their aggregation leads to error cancellation and improved generalization. This relationship is captured by the ensemble error decomposition

| E=e-D | (6) |
| --- | --- |

where Eis the ensemble error, eis the average error of individual models, and Dis the diversity term representing disagreement among models. As discussed in the recent [47] on Aggregation Strategies in Ensemble Regression, maximizing diversity while maintaining individual accuracy is key to ensemble success. This principle underpins ensemble learning’s widespread adoption in domains such as finance, engineering, and scientific forecasting.

### ANN

Neural networks have become indispensable tools for nonlinear regression, offering architectures that transcend the limitations of classical parametric models. Among the earliest and most influential implementations is the General Regression Neural Network (GRNN), introduced by [48],which bypasses iterative training by leveraging radial basis functions and kernel density estimation. GRNN’s architecture—where each training sample corresponds to a neuron—enables rapid learning and robust performance on noisy datasets, though it suffers from scalability issues due to its memory-based nature. In contrast, feedforward neural networks trained via backpropagation remain dominant for general-purpose regression tasks, capable of modeling intricate variable interactions through layered transformations. [49] provides a comparative lens, demonstrating that neural networks outperform traditional regression when data relationships are nonlinear or complex, while regression retains an edge in scenarios with skewed distributions and limited sample sizes. These insights underscore the importance of algorithm selection based on data characteristics and modeling goals.

Beyond predictive accuracy, interpretability has emerged as a critical frontier in neural network regression. ([50]) address this challenge through REFANN (Rule Extraction from Function Approximating Neural Networks), a methodology that distills symbolic rules from trained models by pruning hidden units and approximating their activations with piecewise linear functions. This approach enables the partitioning of input space into interpretable subregions governed by linear rules, bridging the gap between black-box neural models and transparent decision-making. Such rule-based approximations maintain high fidelity to original predictions while offering domain experts a clearer understanding of model behavior. Complementary advances include Bayesian neural networks for uncertainty quantification, ensemble methods for variance reduction, and hybrid architectures that fuse neural learning with fuzzy logic or support vector regression. Together, these developments reflect a rich and evolving landscape—where neural network regression is not merely a modeling technique, but a customizable framework adaptable to diverse operational, interpretive, and computational demands.

### KNN

In the domain of machine learning methods for regression, one notable non-parametric approach is K-Nearest Neighbors (KNN). This instance-based learning method predicts continuous outcomes by averaging the values of the nearest data points. The process can be organized into six key steps [51, 52]:

Step 1: Core Estimation Principle

KNN regression estimates the output for a query point by averaging the outputs of its K closest neighbors in the feature space. The most commonly used distance metric is Euclidean distance, although alternatives such as Manhattan or Mahalanobis distance may be employed depending on the data structure. The prediction rule is typically expressed as:

| y(x)=1Ki=1Kyi | (7) |
| --- | --- |

where yiare the target values of the K nearest neighbors to input x.

Step 2: Selecting the Number of Neighbors (K)

Choosing the appropriate number of neighbors is crucial. A small K makes the model sensitive to noise and results in high variance, while a large K produces smoother predictions but may lead to underfitting. Cross-validation and penalization techniques are commonly used to determine the optimal value of K.

Step 3: Instance Selection and Efficiency

A major challenge in KNN regression is its computational inefficiency with large datasets, which can slow down predictions and increase memory usage. To address this, the DISKR strategy (Decremental Instance Selection for KNN Regression) [53] removes outliers and redundant data points. It applies decremental pruning based on each instance’s contribution to prediction accuracy, thereby improving both speed and storage efficiency.

Step 4: Functional Data Adaptation

When dealing with functional inputs—such as curves, spectra, or time series—a projection process is implemented. Data are mapped onto finite-dimensional subspaces using orthonormal basis functions, allowing KNN to operate effectively in reduced dimensions while preserving the structure of the original functional data.

Step 5: Weighted KNN Regression

To reduce bias from distant neighbors and improve performance in heterogeneous datasets, weights are assigned to neighbors based on their distance from the query point. A common weighting scheme is:

Step 6: Consistency and Theoretical Guarantees

A fundamental concern in KNN regression is consistency—whether the estimator converges to the true regression function as the dataset grows. Small values of K tend to yield low bias but high variance, while larger values increase bias and reduce variance. To balance this trade-off, oracle bounds [54] and other theoretical frameworks provide guarantees on the expected error, guiding the selection of model parameters.

## Accuracy Metrics

Machine learning algorithms are inherently complex, and this complexity grows when datasets contain numerous predictors. The most effective model is the one that accurately represents the underlying phenomenon and produces consistent results under practical conditions. For this reason, the careful selection of evaluation metrics is essential. In fact, more than thirty different metrics have been introduced in the literature, as documented [55]. Recent work further emphasizes that multi‑criteria validation—where several metrics are applied together—provides a more comprehensive and reliable assessment framework [56]. In this study, the key accuracy metrics employed to identify the most effective ML implementation are summarized in Table 2.

Table 2: Key accuracy metrics

| RMSE | Root Mean Squared Error; measures the average magnitude of prediction error. Expressed in the same units as the input data, useful for Gaussian errors | RMSE=1n1nyp- yr2 | [57] |
| --- | --- | --- | --- |
| MAPE | Mean Absolute Percentage Error; provides an intuitive measure of relative error by expressing deviations as percentages of actual values | MAPE=1Ni=1Nyip-yiryir | [58] |
| R2 | Coefficient of Determination) ¦ Indicates the proportion of variance in the dependent variable explained by the model. A higher R² suggests better explanatory power, but it should be considered alongside other metrics | R2= 1-1nyp- yp21nyr- yr2 | [59] |

## Sensitivity analyses

Sensitivity analysis has increasingly emphasized the importance of evaluating the contribution of each input variable to model predictions. To achieve this in a principled way, the SHAP (SHapley Additive exPlanations) framework has been adopted, drawing on the game‑theoretic concept of Shapley values [60]. In cooperative game theory, the Shapley value represents the average marginal contribution of a player to the overall outcome; analogously, in machine learning, the Shapley value of a feature quantifies its contribution to the deviation of a prediction from the model’s average output. For any given query point, the sum of the Shapley values across all features equals the total deviation of the prediction from the mean, thereby ensuring consistency and completeness in the explanation [61]. This property makes SHAP particularly powerful for interpreting complex models such as ensembles or Gaussian process regressors, where accuracy is often achieved at the expense of transparency. By assigning each feature an importance value for individual predictions, SHAP unifies several existing interpretability approaches into a single additive framework with desirable theoretical guarantees. Moreover, extensions such as Kernel SHAP and dependent‑feature SHAP have improved computational efficiency and reliability in cases where predictor correlations may otherwise distort explanations [62]. In the context of this study, SHAP complements traditional sensitivity analysis by providing both local and global insights: locally, it explains how specific parameter values influence individual predictions of surface roughness, while globally, aggregating these local contributions reveals the overall importance ranking of grinding parameters. This dual perspective enhances interpretability, validates the inclusion of novel predictors such as alloy type and coolant type, and guides optimization strategies in machining processes.

## Green Machining Framework Application

To enable user‑friendly and time‑efficient procedures in grinding analysis, the development of digital platforms is essential. Such platforms must support both numerical and algebraic evaluations of experimental data and grinding field parameters. A central feature of these platforms is the creation of fit‑for‑purpose software packages equipped with intuitive, user‑centric graphical user interfaces (GUIs). A major emphasis of the present study is the provision of a comprehensive and universal AI‑based platform for grinding applications. By integrating heterogeneous datasets from multiple sources, this platform ensures flexibility and adaptability across diverse conditions and materials. Most importantly, the final results are designed to connect effectively with end users, and the digital platform presented here offers a practical solution to bridge advanced machine learning methodologies with real‑world industrial applications.

## Structure of Study

The overall structure of this study is organized into four main sections. The first section focuses on data consolidation, which involves preprocessing and preparing datasets. Due to the complexity of this stage, it is described separately to ensure clarity. The second section addresses machine learning (ML) modeling, where different algorithms are applied to capture the relationships between grinding parameters and performance outcomes. The third section presents the accuracy and sensitivity analyses, which are critical for evaluating model performance and identifying the most reliable approaches for subsequent digitalization. Finally, the fourth section introduces the digital platform, which integrates the selected models into a user‑oriented system designed to connect effectively with end users. The complete structure of these four sections is illustrated in Figure 1.

Figure 1: Structure of the study

# Results and Discussion

As part of the multi‑criteria decision‑making (MCDN) procedure, all grinding parameters from the individual studies were first compiled into a comprehensive list. Table 3 presents the complete set of parameters considered during consolidation, including both fixed and variable factors across the Inconel, stainless steel, and aluminum grinding processes. This table highlights the scope of experimental conditions and provides transparency regarding the harmonization process.

However, not all parameters were retained in the final global dataset. To ensure methodological consistency and avoid bias, certain parameters were excluded, as explained in Table 3:

- Grinding mode: Excluded because it was fixed across all studies, consistently defined as down‑surface grinding.

- Grinding machine: Omitted since machine performance depends on intrinsic characteristics not reported in the original studies. Including this parameter could introduce bias. Nevertheless, machine type remains an important factor for future investigations.

- Workpiece dimensions and hardness: Not incorporated because these details were not clearly specified in some datasets, limiting comparability.

- Dresser material: Excluded as it was fixed across all studies, consistently defined as diamond dresser.

- Number of dressing passes: Not considered because this parameter was missing from the aluminum and steel datasets, preventing consistent treatment across materials.

By documenting both the consolidated parameters (Table 3) and the excluded ones with justification (Table 4), the study ensures methodological rigor and transparency. This structured approach strengthens the reliability of the global dataset and provides a clear framework for future extensions, where additional parameters such as grinding machine type may be incorporated once sufficient data are available.

Table 3: Data consolidation of grinding parameters

| Grinding Elements | Inconel 738 (Tables A1–A2) | Steel UNS S34700 (Tables A3–A4) | Aluminium AA6061 (Tables A5–A6) | Cumulative Parameters |
| --- | --- | --- | --- | --- |
| Alloy type | Inconel 738 | UNS S34700 | AA6061 | Variable (Alloy type) |
| Grinding mode | Plunge surface | Down surface grinding | Down surface grinding | Fixed (Surface grinding) |
| Grinding machine | Prompt 300–1000 | M7135A-NANTONG SHUANGZANG | M7135A-NANTONG SHUANGZANG | Excluded |
| Grinding wheel type | Al₂O₃: WA60K9V | 3 wheel types (TYROLIT) | 3 wheel types (TYROLIT) | Variable (Wheel type) |
| Wheel speed (Vs) | 47 m/s | 30 m/s | 30 m/s | Variable (30–47 m/s) |
| Work speed (Vft) | 4.5, 15 m/min | 1500 mm/min | 1500 mm/min | Variable (4.5–1500 mm/min) |
| Depth of grinding / cut | 30 μm (fixed) | 5–65 μm | 5–65 μm | Variable (5–65 μm) |
| Workpiece dimensions | 200 × 40 × 16 mm | Not specified | Not specified | Excluded (unique) |
| Workpiece hardness | Not specified | Hardened stainless steel | 170 HV | Excluded |
| Dresser material | Stationary diamond | Stationary diamond, single point | Stationary diamond, single point | Fixed (Stationary diamond) |
| Dresser type | Single / Four-edge | Single point | Single point | Variable (Single/Four-edge) |
| Number of dressing passes | 3 | Not specified | Not specified | Excluded |
| Dressing feed (Vfd) | 50–600 mm/min | 150 mm/min | 150 mm/min | Variable (50–600 mm/min) |
| Depth of dressing pass (ad) | 2–20 μm | 40 μm | 40 μm | Variable (2–40 μm) |
| Specific removal rate | 135, 450 | 7.5, 22.5, 37.5, 52.5, 67.5, 82.5, 97.5 | 7.5, 22.5, 37.5, 52.5, 67.5, 82.5, 97.5 | Variable (7.5 - 450) |
| Cooling type | Wet, MQL | Dry, MQL1, MQL2, Fluid | Dry, MQL1, MQL2, Fluid | Variable (Dry, Wet (Fluid), MQL, MQL1, MQL2) |

To prepare the data for machine learning implementation, all grinding parameters from the individual studies were consolidated into a single homogeneous dataset. This process was essential for enabling cross‑material comparisons and predictive modeling. While the original datasets contained 17 grinding parameters, the consolidation procedure reduced the number of predictors to 10 variables. This reduction was inevitable, as the primary objective of the study is to ensure flexibility across heterogeneous data sources. Re‑implementing or repeating grinding experiments to fill missing parameters was strictly avoided, since in many cases such re‑testing is impractical or impossible.

The final dataset therefore reflects a balance between methodological rigor and practical feasibility. It ensures that the machine learning models can cope with varied data sources while maintaining comparability across alloys and grinding conditions. Table 4 presents the complete list of input parameters retained as predictors, along with their domains of variation, while surface roughness (Rz) is designated as the target variable. The predictors include workpiece material, cooling method, grinding machine, and dresser properties, in addition to process variables such as wheel speed and depth of cut.

This harmonized dataset provides a robust foundation for model training and evaluation. By capturing the essential variability of grinding behavior while excluding parameters that could introduce bias or inconsistency, the study establishes a reliable framework for multi‑criteria decision making (MCDM). Furthermore, Table 5 provides a snapshot of 10 representative samples from the final dataset, which in total comprises 293 data records. This structured dataset enables both comparative analysis and predictive modeling, extending the scope of grinding research beyond single‑material investigations.

Table 4: Final consolidated dataset variables which will be used in the cumulative study

|  | Grinding Elements | Cumulative Parameters |
| --- | --- | --- |
| Grinding parameters (Predictors) | Alloy type | Inconel™ 738, UNS34700, AA6061 |
|  | Grinding wheel type | Al2O3(WA60K9V), Al2O3 (180K6), Al2O3 (80L6(2)), Al2O3(120I8(8)) |
|  | Wheel speed (Vs) | 30–47 m/s |
|  | Work speed (Vft) | 1.5, 4.5, 15 m/min |
|  | Depth of grinding / cut | 5, 15, 25, 30, 35, 45, 55, 65 μm |
|  | Dresser type | Single/Four-edge |
|  | Dressing feed (Vfd) | 50, 85, 150, 213, 426, 600 mm/min |
|  | Depth of dressing pass (ad) | 2, 5, 10, 20, 40 μm |
|  | Specific removal rate | 7.5, 22.5, 37.5, 52.5, 67.5, 82.5, 97.5, 135, 450 |
|  | Cooling type | Dry, Wet, Fluid, MQL, MQL1, MQL2 |
| Grinding target | Surface roughness (Rz) |  |

Table 5: A snapshot of 10 representative samples from the final dataset

| Alloy Type | Wheel speed | Work speed | Dresser type | Depth of dressing pass | Dressing feed | Depth of grinding | Specific removal rate | Cooling type | Grinding wheel type | Surface roughness (Rz) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 'Steel st304' | 30 | 1.5 | 'Single Point' | 40 | 150 | 15 | 22.5 | 'Dry' | 'Al2O3 80L6(2)' | 1.23 |
| 'Steel st304' | 30 | 1.5 | 'Single Point' | 40 | 150 | 65 | 97.5 | 'Fluid' | 'Al2O3 80L6(2)' | 1.45 |
| 'Inconel 738' | 47 | 15 | 'One point' | 5 | 426 | 30 | 450 | 'Wet' | 'Al2O3 WA60K9V' | 5.085625 |
| 'Steel st304' | 30 | 1.5 | 'Single Point' | 40 | 150 | 55 | 82.5 | 'Fluid' | '120I8(8)' | 1.3 |
| 'Aluminum' | 30 | 1.5 | 'Single Point' | 40 | 150 | 15 | 22.5 | 'Dry' | '120I8(8)' | 0.94 |
| 'Inconel 738' | 47 | 4.5 | 'One point' | 5 | 600 | 30 | 135 | 'Wet' | 'Al2O3 WA60K9V' | 3.425625 |
| 'Inconel 738' | 47 | 15 | 'quadra point' | 5 | 85 | 30 | 450 | 'Wet' | 'Al2O3 WA60K9V' | 5.093125 |
| 'Aluminum' | 30 | 1.5 | 'Single Point' | 40 | 150 | 35 | 52.5 | 'Dry' | 'Al2O3 80L6(2)' | 2.6 |
| 'Steel st304' | 30 | 1.5 | 'Single Point' | 40 | 150 | 5 | 7.5 | 'MQL1' | '120I8(8)' | 0.86 |
| 'Steel st304' | 30 | 1.5 | 'Single Point' | 40 | 150 | 25 | 37.5 | 'MQL1' | '120I8(8)' | 1.03 |

Before implementing machine learning models, it is critical to conduct thorough statistical analysis—ranging from basic measures such as the mean and standard deviation to advanced techniques like N‑Way ANOVA. These analyses provide essential insights into the dataset’s structure, variability, and relationships, ensuring that models are trained on reliable, interpretable, and unbiased data.

The mean captures the central tendency of each variable, offering a benchmark for typical values, while the standard deviation quantifies variability, indicating whether predictors are stable or noisy. Together, these measures reveal whether the dataset is balanced or skewed, guiding preprocessing decisions such as normalization or scaling [63].

Beyond descriptive statistics, N‑Way ANOVA plays a crucial role when multiple factors influence the target variable. It evaluates both the main effects of independent variables (e.g., wheel speed, depth of cut, cooling method) and their interactions—for instance, the effect of cooling method may depend on wheel speed. This approach identifies statistically significant predictors, guides feature selection, and enhances the robustness of machine learning models [64].

By integrating both descriptive and advanced statistical analyses, this study provides a solid foundation for predictive modeling, ensuring that machine learning algorithms are applied to a dataset that is well‑characterized and systematically structured. The outcomes of these intermediate statistical evaluations, which validate the reliability and comparability of the consolidated dataset, are presented in Table 6.

Table 6: Statistical analysis of consolidated dataset

| Grinding parameters | min | max | Average | Standard Deviation | skewness | kurtosis |
| --- | --- | --- | --- | --- | --- | --- |
| Alloy Type | Qualitative variables are categorical and thus excluded from statistical computation |  |  |  |  |  |
| Wheel speed | 30 | 47 | 37.25 | 8.42 | 0.3 | 1.09 |
| Work speed | 1.5 | 15 | 5.22 | 5.51 | 1.13 | 2.45 |
| Dresser type | Qualitative variables are categorical and thus excluded from statistical computation |  |  |  |  |  |
| Depth of dressing pass | 2 | 40 | 27.4 | 15.71 | -0.53 | 1.43 |
| Dressing feed | 50 | 600 | 207.87 | 161.14 | 1.6 | 4.23 |
| Depth of grinding | 5 | 65 | 32.87 | 15.37 | 0.4 | 3.01 |
| Specific removal rate | 7.5 | 450 | 160.8 | 163.93 | 1.08 | 2.43 |
| Cooling type | Qualitative variables are categorical and thus excluded from statistical computation |  |  |  |  |  |
| Grinding wheel type | Qualitative variables are categorical and thus excluded from statistical computation |  |  |  |  |  |
| Surface roughness (Rz) | 0.4 | 7.85 | 2.6 | 1.63 | 0.86 | 3.14 |

Quantitative parameters were examined using a full set of statistical descriptors—including minimum, maximum, mean, standard deviation, skewness, and kurtosis—while qualitative variables were excluded from numerical analysis due to their categorical nature. All of these statistical measures are systematically presented in Table 4, providing a comprehensive overview of the consolidated dataset. This dual approach ensures that the dataset is thoroughly characterized, capturing variability, distributional tendencies, and potential anomalies that must be considered before machine learning implementation.

Wheel speed and grinding depth exhibited relatively low skewness and kurtosis, indicating distributions close to normal and therefore well‑suited for regression‑based modeling. In contrast, work speed, dressing feed, and specific removal rate showed positive skewness and elevated kurtosis, reflecting long‑tailed distributions with possible outliers; such variables may require normalization or transformation prior to machine learning implementation. The depth of dressing pass revealed slight negative skewness, suggesting a bias toward higher values within the dataset.

Surface roughness (Rz), designated as the target variable, demonstrated moderate skewness and kurtosis, implying variability without severe distortion. Meanwhile, categorical parameters such as alloy type, dresser type, cooling method, and wheel type were not subjected to statistical measures but remain critical predictors. These qualitative variables must undergo preprocessing through encoding to be effectively integrated into machine learning models.

The conversion of qualitative parameters—such as coolant type and grinding wheel type—into numerical labels is a necessary preprocessing step for machine learning. Since advanced statistical analyses, including N‑Way ANOVA, and predictive algorithms require numerical inputs, categorical variables must be encoded to enable effective training. This requirement is well established in the literature, as demonstrated in several recent studies [30, 65–67]. In this study, the encoding procedure is summarized in Table 7, which illustrates how categorical parameters were systematically transformed into numerical values to ensure their compatibility with statistical and machine learning models.

Table 7: Data encoding procedure

| Parameter type | Encoding process |
| --- | --- |
| Alloy Type | Inconel 1 ; Aluminum 2; Steel 3 |
| Dresser type | SinglePoint 1; Quadra (Four) Point 4 |
| Cooling type | MLQ 11; Wet 21; Dry 10; MQL1 12; MQL2 13; Fluid 22 |
| Grinding wheel type | Al2O3 WA60K9V 1; Al2O3 180K6 2; Al2O3 80L6(2) 3; Al2O3 120I8(8) 4 |

The N‑Way ANOVA results, presented in Table 8, serve as a valuable statistical filter for identifying significant factors; however, they do not fully capture the complexity of interdependencies within the dataset. The analysis indicates that certain parameters—such as work speed, wheel speed, depth of grinding, and specific removal rate—appear statistically redundant or non‑essential in the current dataset and may be excluded from future analyses. In contrast, alloy type, dressing feed, cooling type, and grinding wheel type demonstrate significant effects, as their p‑values fall below the 5% threshold, and therefore must be considered. Nevertheless, it remains evident that all variables in the dataset contribute to the final surface grinding outcomes. This limitation highlights that ANOVA cannot account for nonlinear or interaction‑driven relationships among parameters. As a result, a complementary strategy is to employ methods capable of modeling such nonlinearities, with machine learning approaches offering a particularly effective solution.

Table 8: N-Way ANOVA analysis results

|  | Sum Sq. | DF | Mean Sq. | F | Prob > F |
| --- | --- | --- | --- | --- | --- |
| Alloy Type | 6.660 | 1 | 6.660 | 11.804 | 7.E-04 |
| Wheel speed | 0.000 | 0 | 0.000 | 0.000 | NaN |
| Work speed | 0.000 | 0 | 0.000 | 0.000 | NaN |
| Dresser type | 0.336 | 1 | 0.336 | 0.596 | 4.E-01 |
| Depth of dressing pass | 2.639 | 5 | 0.528 | 0.936 | 5.E-01 |
| Dressing feed | 21.917 | 4 | 5.479 | 9.711 | 2.E-07 |
| Depth of grinding | 0.000 | 0 | 0.000 | 0.000 | NaN |
| Specific removal rate | 0.000 | 0 | 0.000 | 0.000 | NaN |
| Cooling type | 18.931 | 4 | 4.733 | 8.388 | 2.E-06 |
| Grinding wheel type | 14.527 | 2 | 7.264 | 12.873 | 5.E-06 |
| Error | 150.654 | 267 | 0.564 |  |  |
| Total | 780.245 | 292 |  |  |  |

The machine learning results of the current study are presented through both graphical and tabular analyses. Following the data encoding stage, hyperparameter optimization was performed using a Bayesian approach implemented in MATLAB. To ensure a more robust training process and to mitigate both underfitting and overfitting, a 5‑fold cross‑validation strategy was applied across all models. The optimized hyperparameter values for the five implemented algorithms—Support Vector Regression (SVR), Gaussian Process Regression (GPR), Artificial Neural Networks (ANN), Ensemble methods, and k‑Nearest Neighbors (KNN)—are summarized in Table 9.

The training and testing outcomes for each model are illustrated in Figures 2–6, where alloy types are distinguished by color: Inconel in black, Aluminum in green, and Steel in red. In these figures, the horizontal axis represents the actual surface roughness values, while the vertical axis shows the predicted values, first for training and then for testing. Ideally, the best predictive performance is achieved when all data points align closely with the perfect prediction line.

From the visual inspection of these results, the Ensemble model and, to a lesser extent, the GPR model provided superior predictions with minimal variation. In contrast, the ANN model exhibited the greatest dispersion, indicating weaker predictive capability. A notable challenge across all models was the strong fluctuation observed in the Inconel 738 data, which led to severe dispersion and reduced prediction accuracy for this alloy. Despite this difficulty, the Ensemble model consistently delivered the most reliable results across all alloy types.

Nevertheless, conclusions drawn solely from graphical analysis are insufficient. To provide a more rigorous evaluation, the accuracy metrics for all models are reported in Table 10, offering a quantitative comparison of their predictive performance.

Table 9: Optimized machine hyperparameters

| ML Models | Hyperparameters | Search Space | Optimal Values |
| --- | --- | --- | --- |
| SVR | C | (0.1, 100) | 1.915 |
|  | Epsilon | (0.01, 10) | 0.1915 |
|  | Kernel function | polynomial, Gaussian | Gaussian |
| GPR | Sigma | (0.01, 10) | 3.2314 |
|  | Kernel function | RQ, SE, M52, Exp. | RQ |
| ANN | Hidden layers | 1,2,3 | 2 |
|  | Neurons in each layer | (5, 200) | 30, 100 |
|  | Learning rate | [0.01, 1] | 1 |
|  | Activation function | Relu, Sigmoid, tanh | Relu |
| Ensemble | Ensemble algorithm | Bag, LSBoost | LSBoost |
|  | Number of weak learners | (1, 20) | 5 |
|  | Learning rate | (0.01, 1) | 0.1 |
| KNN | Number of neighbors | (2, 200) | 9 |

| Figure 2: Final results of SVR method implementations on the cumulative data (left treaining and right is related to test procedure) |  |
| --- | --- |

| Figure 3: Final results of GPR method implementations on the cumulative data (left treaining and right is related to test procedure) |  |
| --- | --- |

| Figure 4: Final results of Ensemble method implementations on the cumulative data (left training and right is related to test procedure) |  |
| --- | --- |

| Figure 5: Final results of ANN method implementations on the cumulative data (left training and right is related to test procedure) |  |
| --- | --- |

| Figure 6: Final results of KNN method implementations on the cumulative data (left training and right is related to test procedure) |  |
| --- | --- |

The comparative performance of the machine learning models is summarized in Table 10, which reports accuracy, RMSE, R², and MAPE for both the training and testing phases across the complete dataset and the three evaluated alloys.

Table 10: Final models accuracy metrics report

| Procedure | Models | Metrics | Total | Inconel | Aluminium | Steel |
| --- | --- | --- | --- | --- | --- | --- |
| Training | SVR | Accuracy (%) | 81 | 81 | 81 | 81 |
|  |  | RMSE | 0.74 | 1.07 | 0.40 | 0.26 |
|  |  | R2 | 0.79 | 0.21 | 0.75 | 0.59 |
|  |  | MAPE (%) | 19.03 | 18.99 | 19.19 | 18.94 |
|  | GPR | Accuracy (%) | 80 | 80 | 79 | 81 |
|  |  | RMSE | 0.72 | 1.02 | 0.43 | 0.26 |
|  |  | R2 | 0.80 | 0.28 | 0.70 | 0.60 |
|  |  | MAPE (%) | 19.87 | 19.63 | 21.36 | 18.72 |
|  | Ensemble | Accuracy (%) | 85 | 80 | 86 | 90 |
|  |  | RMSE | 0.72 | 1.05 | 0.36 | 0.16 |
|  |  | R2 | 0.80 | 0.24 | 0.79 | 0.85 |
|  |  | MAPE (%) | 15.32 | 19.64 | 14.19 | 10.03 |
|  | ANN | Accuracy (%) | 76 | 63 | 86 | 86 |
|  |  | RMSE | 1.31 | 1.99 | 0.25 | 0.26 |
|  |  | R2 | 0.34 | -1.73 | 0.90 | 0.60 |
|  |  | MAPE (%) | 23.81 | 37.16 | 13.71 | 14.07 |
|  | KNN | Accuracy (%) | 69 | 74 | 59 | 73 |
|  |  | RMSE | 1.11 | 1.52 | 0.83 | 0.46 |
|  |  | R2 | 0.52 | -0.60 | -0.09 | -0.28 |
|  |  | MAPE (%) | 30.56 | 26.37 | 40.74 | 26.62 |
| Testing | SVR | Accuracy (%) | 78 | 80 | 75 | 79 |
|  |  | RMSE | 0.983 | 1.474 | 0.238 | 0.259 |
|  |  | R2 | 0.680 | -0.399 | 0.748 | 0.526 |
|  |  | MAPE (%) | 21.734 | 20.147 | 24.613 | 21.237 |
|  | GPR | Accuracy (%) | 71 | 82 | 57 | 68 |
|  |  | RMSE | 0.832 | 1.195 | 0.405 | 0.338 |
|  |  | R2 | 0.771 | 0.080 | 0.270 | 0.192 |
|  |  | MAPE (%) | 29.130 | 18.117 | 42.740 | 32.039 |
|  | Ensemble | Accuracy (%) | 83 | 85 | 75 | 88 |
|  |  | RMSE | 0.718 | 1.065 | 0.280 | 0.151 |
|  |  | R2 | 0.830 | 0.270 | 0.651 | 0.838 |
|  |  | MAPE (%) | 17.382 | 15.420 | 25.188 | 12.518 |
|  | ANN | Accuracy (%) | 71 | 54 | 83 | 83 |
|  |  | RMSE | 1.649 | 2.495 | 0.358 | 0.315 |
|  |  | R2 | -0.046 | -3.314 | 0.795 | 0.399 |
|  |  | MAPE (%) | 29.341 | 46.178 | 16.881 | 16.779 |
|  | KNN | Accuracy (%) | 63 | 70 | 40 | 76 |
|  |  | RMSE | 1.291 | 1.874 | 0.673 | 0.332 |
|  |  | R2 | 0.448 | -1.262 | -1.017 | 0.220 |
|  |  | MAPE (%) | 37.035 | 30.291 | 60.412 | 23.774 |

Examining the Total metrics, the Ensemble model consistently emerges as the most reliable predictor of surface roughness. It demonstrates the highest accuracy in both training (85%) and testing (83%) while simultaneously achieving the lowest RMSE and MAPE values and the strongest R² performance. GPR follows as the second-best model, exhibiting smooth and stable behavior with balanced accuracy and R² scores. SVR shows moderate but steady performance, while ANN and KNN lag behind, reflecting reduced capacity to capture the nonlinear behavior inherent in grinding processes.

A comparison between the training and testing stages offers insight into model generalization. The Ensemble model exhibits excellent robustness, with minimal degradation in all performance metrics when evaluated on unseen data. SVR similarly maintains stable behavior, confirming its suitability for applications where consistency is prioritized. GPR shows a modest decline in testing accuracy yet retains comparatively high R² values, indicating that it generalizes reasonably well despite sensitivity to data irregularities. In contrast, ANN and KNN display considerable performance deterioration, especially visible in their R² and MAPE values. These trends indicate that both models tend to overfit the training data and are less capable of adapting to new, previously unseen operating conditions.

The alloy-specific evaluations further highlight the variability in predictive difficulty across materials. Inconel 738 consistently exhibits the poorest predictive outcomes across all models, with markedly low or even negative R² values, elevated RMSE, and substantially higher MAPE levels. This quantitative evidence aligns with the observed experimental fluctuations in the Inconel dataset and confirms its status as the most challenging material to model. Aluminum, by contrast, emerges as the most predictable alloy, yielding the highest R² values and the lowest error metrics across most models. Steel performs similarly well, showing stable and accurate predictions but with slightly higher variance than Aluminum. Collectively, the results underscore the strong material dependence of the grinding process, highlighting that model performance is heavily influenced by the inherent stability and variability of each alloy’s response.

## Taylor Diagram

From the previous section, the process of selecting the best model for further implementation was based on the separate analysis of accuracy metrics. However, as emphasized in Section 2.5, the identification of the optimal model should rely on a multidisciplinary approach. For this reason, several multidimensional visual evaluation methods—such as the Taylor diagram [68], ARAS diagram [69], and Target diagram [70]—were introduced. These methods allow simultaneous consideration of different accuracy metrics (including standard deviation, root mean square error, and correlation coefficient) within a single visual framework, thereby facilitating a more comprehensive model selection process [71, 72].

Among these evaluation techniques, the Taylor diagram was selected due to its ability to integrate multiple statistical measures, as discussed earlier, and its established use as a well-recognized method in the field of artificial intelligence. The results of the Taylor diagram analysis for the current study are illustrated in Figures 7 and 8. Figure 7 presents the combined dataset, where both training and testing outputs were merged into a single universal dataset. The diagram clearly shows that the GPR and Ensemble models, with their higher R2values, lower standard deviations, and RMSD values closer to the actual Rz, exhibit superior performance. While SVR and KNN also demonstrate acceptable results, they do not outperform Ensemble and GPR. By contrast, the ANN model fails to adequately capture the complexity of the universal dataset, resulting in poor predictive accuracy.

Figure 8 highlights the novelty of this study by introducing workpiece alloy type as a primary evaluation criterion. The Taylor diagrams for Inconel, Aluminum, and Steel alloys are illustrated separately. The results indicate that the Ensemble method, which integrates multiple machine learning approaches, performs best for Steel and Aluminum datasets. However, due to the high complexity and severe data variation associated with Inconel 738, the GPR model provides the most reliable predictions, followed by the Ensemble method, which still delivers acceptable results.

Figure 7: Taylor diagram for all models conducted on consolidated dataset

| - Inconel | - Aluminum | - Steel |
| --- | --- | --- |
| Figure 8: Taylor diagram for all models conducted on consolidated dataset with separation on types of alloy |  |  |

## Sensitivity Analysis

SHAP (SHapley Additive exPlanations) analysis was applied to the two best-performing models – Ensemble and Gaussian Process Regression (GPR) – with  the results presented in Figures 9 and 10, respectively. This analysis provides a transparent, game‑theoretic framework for quantifying the contribution of each predictor to the predicted surface roughness. Both models highlight a consistent set of dominant predictors, confirming the robustness of the feature selection process. Specifically, Specific Removal Rate, Grinding Wheel Type, and Dressing Speed emerge as the most influential parameters, while Types of Alloy and Coolant Type also demonstrate substantial contributions, validating their inclusion as novel variables in this study.

The plots further reveal the directional impact of predictors. In both models, high Wheel Speed is strongly associated with increased surface roughness, as indicated by positive SHAP values concentrated on the right side of the distribution for higher feature values (yellow points). Conversely, low Specific Removal Rate and low Dressing Speed are linked to reductions in surface roughness, reflected by negative SHAP values and lower feature values (blue points). These relationships highlight the dual role of process parameters: while aggressive operating conditions may elevate roughness, controlled removal rates and dressing speeds can mitigate it.

Comparing the two models, the Ensemble method provides a clearer separation of feature importance, with more distinct SHAP value ranges across predictors. This enhances interpretability and makes it easier to identify which parameters exert the strongest influence under varying operating conditions. The GPR model, while slightly less distinct in its separation, captures subtle nonlinear interactions among mid‑ranked features such as Workspeed and Depth of Dressing, offering a complementary perspective on parameter behavior. Together, these results demonstrate that both models converge on the same critical predictors, but the Ensemble model offers superior clarity in ranking and visualization, supporting its selection as the preferred approach for practical deployment.

Figure 9: SHAP analysis results on Ensemble model

Figure 10: SHAP analysis results on GPR model

## Green Machining Framework Application

The final step in the analysis procedure involves the development of a user‑friendly interface application that integrates all previous components into a unified, general‑purpose platform. This application enhances both algebraic analysis and predictive modeling of field and experimental data, thereby accelerating the overall evaluation process. A key aspect of such platforms is the creation of fit‑for‑purpose software packages that are compatible with multiple operating systems (e.g., Windows and macOS). As illustrated in Figure 16, the macOS‑compatible version of the application is shown; however, the interface remains consistent across both platforms.

The platform is structured in multiple layers. The initial layer – the backend – contains the predefined dataset used in this study. It is also designed to accept new datasets and can connect to SQL‑based databases, thereby increasing flexibility and universality. Furthermore, the backend incorporates all machine learning models discussed in the study. The analysis procedure involves training the models on the dataset, testing their performance, selecting the best‑performing algorithm, and reporting the results through the user interface, as demonstrated in Figure 16.

The next layer is the front‑end, which allows users to input their own values for the grinding parameters. Based on the current study, the interface includes ten grinding parameters, reflecting the scope of the dataset. End‑users can select their desired input values, and the software—using the best‑trained and selected model—predicts the corresponding surface roughness. It is important to note that the predicted surface roughness is an estimated value based on the selected model and reflects the average accuracy of that model.

This layered architecture ensures efficient data processing and intuitive user interaction, ultimately enhancing the usability and functionality of the software. It should be noted that the development of this Green Machining Framework Application, while grounded in machine learning concepts, is not cloud‑based due to data privacy concerns and institutional policies set by the data source provider.

Figure 11: GUI of green machining framework

# Conclusion

The foundation of this study was built upon the central question of whether alloy type, when considered alongside conventional grinding parameters, exerts a measurable influence on the final surface roughness quality. To address this phenomenon, three distinct grinding datasets—each extensively studied within the domain of machine learning and conducted on different workpiece alloys—were harmonized into a single, universal dataset. This consolidation was achieved through a structured multi‑criteria decision‑making (MCDM) framework, designed to ensure consistency and comparability across datasets. The framework was guided by five key rules: (i) alloy type is treated as a variable, (ii) each dataset defines its own fixed and variable parameters, (iii) if a parameter varies in any dataset it is treated as variable, (iv) a parameter is considered fixed only if it remains constant across all datasets, and (v) parameters unique to one dataset but absent in others are excluded.

Applying these rules to the original 16 grinding parameters resulted in a consolidated dataset containing 10 core variables: alloy type, wheel speed, work speed, dresser type, depth of dressing pass, dressing feed, depth of grinding, specific removal rate, cooling type, and grinding wheel type, with surface roughness (Rz) serving as the response variable. This harmonization not only ensured methodological rigor but also created a robust and universal dataset capable of capturing the combined influence of both traditional grinding parameters and the newly introduced alloy type variable. By establishing this consolidated dataset, the study provided a reliable foundation for subsequent machine learning implementation and interpretability analysis.

In the second stage, machine learning techniques were applied to the consolidated dataset. A comprehensive preprocessing procedure was first conducted, including fundamental and intermediate statistical analyses to provide an overview of the dataset’s structure. To enable advanced statistical evaluation, qualitative variables were encoded into quantitative form, allowing the implementation of N-Way ANOVA. However, the ANOVA results misleadingly suggested that parameters such as wheel speed, work speed, and depth of grinding exerted little influence on surface roughness. This conclusion contradicts well-established physical principles of grinding, thereby highlighting the limitations of ANOVA in capturing complex nonlinear relationships among parameters. Consequently, the adoption of advanced machine learning models was deemed necessary to uncover more reliable and interpretable patterns.

Five machine learning algorithms were considered: Support Vector Regression (SVR), Gaussian Process Regression (GPR), Artificial Neural Networks (ANN), Ensemble methods, and k-Nearest Neighbors (KNN). Following adaptive hyperparameter tuning using a Bayesian optimization approach, each model was trained and tested on the consolidated dataset. Among them, the Ensemble model achieved the highest performance, with an R2value of 0.80 and mean accuracy of 85% during training, and an R2of 0.83 with 83% mean accuracy during testing. The GPR model also performed competitively, with R2values of 0.80 and 0.77 for training and testing, respectively, ranking as the second-best model. These results confirm the superiority of machine learning approaches over traditional statistical methods in modeling the grinding process and demonstrate the Ensemble model’s robustness as the most effective predictive tool in this study.

The third stage focused on validating the performance of the implemented machine learning models and interpreting their predictive behavior. To confirm the best models, a Taylor diagram was employed, which clearly demonstrated that both the Ensemble and GPR models exhibited the shortest distance to the reference point of surface roughness (Rz) on the vertical axis. This result reinforced their superior accuracy and reliability compared to the other candidate models.

Following model validation, SHAP (SHapley Additive exPlanations) analysis was conducted to perform sensitivity analysis and identify the parameters exerting the greatest influence on surface roughness. This process was crucial for uncovering direct relationships between grinding parameters and the final surface quality. The findings revealed that Specific Removal Rate, Grinding Wheel Type, and Dressing Speed consistently ranked among the most influential features across both models. Moreover, Types of Alloy and Coolant Type also demonstrated strong contributions, thereby validating their inclusion as novel predictors in this study. These results highlight the importance of integrating both traditional and newly introduced parameters into predictive modeling frameworks, ensuring a more comprehensive understanding of the grinding process and its impact on surface roughness.

At the final stage of the study, a comprehensive software platform was developed to integrate all processes conducted throughout the research into a unified system. The backend of this platform consolidates the harmonized dataset, machine learning models, and sensitivity analysis procedures, thereby serving as the computational core of the framework. On top of this, a user‑friendly graphical interface was implemented to enhance accessibility and universality, enabling seamless interaction with the models and data. The interface allows users to input grinding parameters, query predictions of surface roughness, and explore the influence of different variables, thus bridging the gap between advanced machine learning methods and practical industrial use.

This layered architecture not only supports the combination of data from multiple sources but also provides a scalable use case for future applications in machining optimization. By embedding the validated Ensemble and GPR models within the platform, the system ensures reliable predictions while maintaining interpretability through SHAP‑based sensitivity analysis. The resulting Green Machining Framework Application represents a practical step toward intelligent manufacturing, offering a versatile tool for researchers and practitioners to evaluate, optimize, and extend grinding processes in alignment with sustainability and efficiency goals.

The future direction of this study lies in expanding the scope of the consolidated dataset by incorporating additional data from diverse sources and machining conditions. Integrating larger and more heterogeneous datasets will strengthen the universality of the framework and improve its applicability across different industrial contexts. Furthermore, the adoption of more advanced and sophisticated machine learning algorithms, capable of capturing complex nonlinear interactions with higher accuracy, will enhance predictive performance and reliability. These improvements will support the transition of the developed application from a research‑oriented tool into a fully deployable industrial solution. Ultimately, the goal is to implement the Green Machining Framework Application within real manufacturing environments, enabling practitioners to optimize grinding processes, improve surface quality, and align machining practices with sustainability and efficiency objectives.

References

1. 	Marinescu ID (2013) Tribology of abrasive machining processes, 2nd edition. Elsevier/WA, Amsterdam

2. 	Rowe WB (2014) Principles of modern grinding technology, 2nd edition. William Andrew, Amsterdam

3. 	Poulachon G, Bandyopadhyay BP, Jawahir IS, et al (2003) The influence of the microstructure of hardened tool steel workpiece on the wear of PCBN cutting tools. International Journal of Machine Tools and Manufacture 43:139–144. https://doi.org/10.1016/S0890-6955(02)00170-0

4. 	Aurich JC, Dornfeld D, Arrazola PJ, et al (2009) Burrs—Analysis, control and removal. CIRP Annals 58:519–542. https://doi.org/10.1016/j.cirp.2009.09.004

5. 	Hadad M, Sharbati A (2017) Analysis of the effects of dressing and wheel topography on grinding process under different coolant-lubricant conditions. Int J Adv Manuf Technol 90:3727–3738. https://doi.org/10.1007/s00170-016-9703-0

6. 	Montgomery DC (2020) Design and analysis of experiments, Tenth edition, EMEA edition. Wiley, Hoboken, NJ

7. 	Dehghanpour Abyaneh M, Narimani P, Hadad M, Attarsharghi S (2023) Using machine learning and optimization for controlling surface roughness in grinding of St37. Energy Equip Syst 11:. https://doi.org/10.22059/ees.2023.2000614.1424

8. 	Wuest T, Weimer D, Irgens C, Thoben K-D (2016) Machine learning in manufacturing: advantages, challenges, and applications. Production & Manufacturing Research 4:23–45. https://doi.org/10.1080/21693277.2016.1192517

9. 	Svozil D, Kvasnicka V, Pospichal J (1997) Introduction to multi-layer feed-forward neural networks. Chemometrics and Intelligent Laboratory Systems 39:43–62. https://doi.org/10.1016/S0169-7439(97)00061-0

10. 	Pan Y, Zhou P, Yan Y, et al (2021) New insights into the methods for predicting ground surface roughness in the age of digitalisation. Precision Engineering 67:393–418. https://doi.org/10.1016/j.precisioneng.2020.11.001

11. 	Chandrasekaran M, Devarasiddappa D (2014) Artificial neural network modeling for surface roughness prediction in cylindrical grinding of Al-SiCp metal matrix composites and ANOVA analysis. Adv produc engineer manag 9:59–70. https://doi.org/10.14743/apem2014.2.176

12. 	Govindhasamy JJ, McLoone SF, Irwin GW, et al (2005) Neural modelling, control and optimisation of an industrial grinding process. Control Engineering Practice 13:1243–1258. https://doi.org/10.1016/j.conengprac.2004.11.006

13. 	Rasmussen CE, Williams CKI (2005) Gaussian Processes for Machine Learning. The MIT Press

14. 	Smola AJ, Schölkopf B (2004) A tutorial on support vector regression. Statistics and Computing 14:199–222. https://doi.org/10.1023/B:STCO.0000035301.49549.88

15. 	Shang S, Wang C, Liang X, et al (2023) Surface Roughness Prediction in Ultra-Precision Milling: An Extreme Learning Machine Method with Data Fusion. Micromachines 14:2016. https://doi.org/10.3390/mi14112016

16. 	Bai L, Yang Q, Cheng X, et al (2023) A hybrid physics-data-driven surface roughness prediction model for ultra-precision machining. Sci China Technol Sci 66:1289–1303. https://doi.org/10.1007/s11431-022-2358-4

17. 	Ruan P, Saxena D, Cao J, et al (2025) NASPrecision: Neural Architecture Search-Driven Multi-Stage Learning for surface roughness prediction in ultra-precision machining. Expert Systems with Applications 262:125540. https://doi.org/10.1016/j.eswa.2024.125540

18. 	Shehzad A, Rui X, Ding Y, et al (2024) Deep-learning-assisted online surface roughness monitoring in ultraprecision fly cutting. Sci China Technol Sci 67:1482–1497. https://doi.org/10.1007/s11431-023-2615-4

19. 	Sizemore NE, Nogueira ML, Greis NP, Davies MA (2022) Application of machine learning for improved surface quality classification in ultra-precision machining of germanium. Journal of Manufacturing Systems 65:296–316. https://doi.org/10.1016/j.jmsy.2022.09.001

20. 	Balonji S, Tartibu LK, Okokpujie IP (2023) Prediction Analysis of Surface Roughness of Aluminum Al6061 in End Milling CNC Machine Using Soft Computing Techniques. Applied Sciences 13:4147. https://doi.org/10.3390/app13074147

21. 	Abbas AT, Sharma N, Al-Bahkali EA, et al (2023) A Machine Learning Perspective to the Investigation of Surface Integrity of Al/SiC/Gr Composite on EDM. JMMP 7:163. https://doi.org/10.3390/jmmp7050163

22. 	Gurgenc T, Altay O (2022) Surface roughness prediction of wire electric discharge machining (WEDM)-machined AZ91D magnesium alloy using multilayer perceptron, ensemble neural network, and evolving product-unit neural network. Materials Testing 64:350–362. https://doi.org/10.1515/mt-2021-2034

23. 	Uçar F, Kati N (2020) MACHINE LEARNING BASED PREDICTIVE MODEL FOR SURFACE ROUGHNESS IN CYLINDRICAL GRINDING OF AL BASED METAL MATRIX COMPOSITE. European Journal of Technic. https://doi.org/10.36222/ejt.773093

24. 	Samavatian M, Samavatian V, Kanabar B, et al (2025) Analytically guided machine learning for surface roughness determination in steel grinding processes. Ironmaking & Steelmaking: Processes, Products and Applications 03019233251357108. https://doi.org/10.1177/03019233251357108

25. 	Bailly A, Blanc C, Francis É, et al (2022) Effects of dataset size and interactions on the prediction performance of logistic regression and deep learning models. Computer Methods and Programs in Biomedicine 213:106504. https://doi.org/10.1016/j.cmpb.2021.106504

26. 	Hadad M, Makarian J (2021) Experimental investigation of the effects of dressing and coolant-lubricant conditions on grinding of Nickel-based superalloy-Inconel 738. Energy Equip Syst 9:. https://doi.org/10.22059/ees.2021.243054

27. 	Gupta MK, Khan AM, Song Q, et al (2021) A review on conventional and advanced minimum quantity lubrication approaches on performance measures of grinding process. Int J Adv Manuf Technol 117:729–750. https://doi.org/10.1007/s00170-021-07785-x

28. 	Prashanth GS, Sekar P, Bontha S, Balan ASS (2023) Grinding parameters prediction under different cooling environments using machine learning techniques. Materials and Manufacturing Processes 38:235–244. https://doi.org/10.1080/10426914.2022.2116043

29. 	Hadad M, Attarsharghi S, Dehghanpour Abyaneh M, et al (2024) Exploring New Parameters to Advance Surface Roughness Prediction in Grinding Processes for the Enhancement of Automated Machining. JMMP 8:41. https://doi.org/10.3390/jmmp8010041

30. 	Dehghanpour Abyaneh M, Narimani P, Javadi MS, et al (2024) Predicting Surface Roughness and Grinding Forces in UNS S34700 Steel Grinding: A Machine Learning and Genetic Algorithm Approach to Coolant Effects. Physchem 4:495–523. https://doi.org/10.3390/physchem4040035

31. 	Abyaneh MD, Javadi MS, Narimani P, et al (2025) Enhancing Grinding Efficiency in Aluminum Alloys: An Ensemble‑Stacking and Single Machine Learning Framework for Predicting Surface Roughness with SHAP-based interpretability

32. 	Köhler J (2014) Grinding Parameters. In: The International Academy for Production Engineering, Laperrière L, Reinhart G (eds) CIRP Encyclopedia of Production Engineering. Springer Berlin Heidelberg, Berlin, Heidelberg, pp 597–601

33. 	Zhang Y, Gong P, Tang L, et al (2024) Topography Modeling of Surface Grinding Based on Random Abrasives and Performance Evaluation. Chin J Mech Eng 37:93. https://doi.org/10.1186/s10033-024-01081-x

34. 	Rodriguez RL, Lopes JC, Garcia MV, et al (2020) Grinding process applied to workpieces with different geometries interrupted using CBN wheel. Int J Adv Manuf Technol 107:1265–1275. https://doi.org/10.1007/s00170-020-05122-2

35. 	Chowdhury SR, Chatterjee S, Chakraborty S (2024) Optimization of grinding processes using multi-criteria decision making methods in intuitionistic fuzzy environment. OPSEARCH 61:709–740. https://doi.org/10.1007/s12597-024-00741-9

36. 	Zhang Y, Xiao G, Gao H, et al (2022) Roughness Prediction and Performance Analysis of Data-Driven Superalloy Belt Grinding. Front Mater 9:765401. https://doi.org/10.3389/fmats.2022.765401

37. 	Fu X, Lv L, Chen B, et al (2024) Pre-control of grinding surface quality by data-driven: a review. Int J Adv Manuf Technol 133:3081–3104. https://doi.org/10.1007/s00170-024-13921-0

38. 	Zhang F, O’Donnell LJ (2020) Support vector regression. In: Machine Learning. Elsevier, pp 123–140

39. 	Awad M, Khanna R (2015) Support Vector Regression. In: Efficient Learning Machines. Apress, Berkeley, CA, pp 67–80

40. 	Azizi A, Rooki R, Mollayi N (2020) Modeling and prediction of wear rate of grinding media in mineral processing industry using multiple kernel support vector machine. SN Appl Sci 2:1469. https://doi.org/10.1007/s42452-020-03212-0

41. 	Rasmussen CE, Williams CKI (2008) Gaussian processes for machine learning. In: Gaussian processes for machine learning, 3. print. MIT Press, Cambridge, Mass., pp 7–30

42. 	Seeger M (2004) GAUSSIAN PROCESSES FOR MACHINE LEARNING. Int J Neur Syst 14:69–106. https://doi.org/10.1142/S0129065704001899

43. 	Kanagawa M, Hennig P, Sejdinovic D, Sriperumbudur BK (2018) Gaussian Processes and Kernel Methods: A Review on Connections and Equivalences

44. 	Qiu X, Zhang L, Ren Y, et al (2014) Ensemble deep learning for regression and time series forecasting. In: 2014 IEEE Symposium on Computational Intelligence in Ensemble Learning (CIEL). IEEE, Orlando, FL, USA, pp 1–6

45. 	Dietterich TG (2002) Ensemble learning. The handbook of brain theory and neural networks 2:110–125

46. 	Kunapuli G (2023) Ensemble methods for machine learning. Manning, Shelter Island, NY

47. 	Ardabili S, Mosavi A, Várkonyi-Kóczy AR (2019) Advances in Machine Learning Modeling Reviewing Hybrid and Ensemble Methods

48. 	Specht DF (1991) A general regression neural network. IEEE Trans Neural Netw 2:568–576. https://doi.org/10.1109/72.97934

49. 	Kumar U (2005) Comparison of neural networks and regression analysis: A new insight. Expert Systems with Applications 29:424–430. https://doi.org/10.1016/j.eswa.2005.04.034

50. 	Setiono R, Wee Kheng Leow, Zurada JM (2002) Extraction of rules from artificial neural networks for nonlinear regression. IEEE Trans Neural Netw 13:564–577. https://doi.org/10.1109/TNN.2002.1000125

51. 	Song Y, Liang J, Lu J, Zhao X (2017) An efficient instance selection algorithm for k nearest neighbor regression. Neurocomputing 251:26–34. https://doi.org/10.1016/j.neucom.2017.04.018

52. 	Kramer O (2013) K-Nearest Neighbors. In: Dimensionality Reduction with Unsupervised Nearest Neighbors. Springer Berlin Heidelberg, Berlin, Heidelberg, pp 13–23

53. 	Singh H, Subramanyam AV, Rajput S, Kankanhalli M (2025) Nearest Neighbor Projection Removal Adversarial Training

54. 	Laloë T (2008) A k-nearest neighbor approach for functional regression. Statistics & Probability Letters 78:1189–1193. https://doi.org/10.1016/j.spl.2007.11.014

55. 	Naser MZ, Alavi AH (2023) Error Metrics and Performance Fitness Indicators for Artificial Intelligence and Machine Learning in Engineering and Sciences. Archit Struct Constr 3:499–517. https://doi.org/10.1007/s44150-021-00015-8

56. 	Narimani P, Abyaneh MD, Golabchi M, et al (2024) Digitalization of Analysis of a Concrete Block Layer Using Machine Learning as a Sustainable Approach. Sustainability 16:7591. https://doi.org/10.3390/su16177591

57. 	Hodson TO (2022) Root-mean-square error (RMSE) or mean absolute error (MAE): when to use them or not. Geosci Model Dev 15:5481–5487. https://doi.org/10.5194/gmd-15-5481-2022

58. 	Chicco D, Warrens MJ, Jurman G (2021) The coefficient of determination R-squared is more informative than SMAPE, MAE, MAPE, MSE and RMSE in regression analysis evaluation. PeerJ Computer Science 7:e623. https://doi.org/10.7717/peerj-cs.623

59. 	Kvålseth TO (1985) Cautionary Note about R2. The American Statistician 39:279–285. https://doi.org/10.1080/00031305.1985.10479448

60. 	Lundberg SM, Lee S-I (2017) A Unified Approach to Interpreting Model Predictions. In: Advances in Neural Information Processing Systems. Curran Associates, Inc.

61. 	Lundberg SM, Erion G, Chen H, et al (2020) From local explanations to global understanding with explainable AI for trees. Nat Mach Intell 2:56–67. https://doi.org/10.1038/s42256-019-0138-9

62. 	Aas K, Jullum M, Løland A (2021) Explaining individual predictions when features are dependent: More accurate approximations to Shapley values. Artificial Intelligence 298:103502. https://doi.org/10.1016/j.artint.2021.103502

63. 	Ibrahimi E, Lopes MB, Dhamo X, et al (2023) Overview of data preprocessing for machine learning applications in human microbiome research. Front Microbiol 14:1250909. https://doi.org/10.3389/fmicb.2023.1250909

64. 	Abdumalikov S, Kim J, Yoon Y (2024) Performance Analysis and Improvement of Machine Learning with Various Feature Selection Methods for EEG-Based Emotion Classification. Applied Sciences 14:10511. https://doi.org/10.3390/app142210511

65. 	Prashanth GS, Sekar P, Bontha S, Balan ASS (2023) Grinding parameters prediction under different cooling environments using machine learning techniques. Materials and Manufacturing Processes 38:235–244. https://doi.org/10.1080/10426914.2022.2116043

66. 	Hu Z, Chen H, Zhang K, Wei H (2025) Model-Based Prediction of Grinding Surface Roughness With Error Correction via a Knowledge-Based Fuzzy Broad Learning System. IEEE Trans Instrum Meas 74:1–14. https://doi.org/10.1109/TIM.2025.3574910

67. 	Hu Z, Wang T, Chen H, et al (2025) Physics-Guided Meta-Learning for Surface Roughness Prediction Under Various Working Conditions With Limited Data. IEEE/ASME Trans Mechatron 1–11. https://doi.org/10.1109/TMECH.2025.3598351

68. 	Taylor KE (2001) Summarizing multiple aspects of model performance in a single diagram. J Geophys Res 106:7183–7192. https://doi.org/10.1029/2000JD900719

69. 	Izzaddin A, Langousis A, Totaro V, et al (2024) A new diagram for performance evaluation of complex models. Stoch Environ Res Risk Assess 38:2261–2281. https://doi.org/10.1007/s00477-024-02678-3

70. 	Jolliff JK, Kindle JC, Shulman I, et al (2009) Summary diagrams for coupled hydrodynamic-ecosystem model skill assessment. Journal of Marine Systems 76:64–82. https://doi.org/10.1016/j.jmarsys.2008.05.014

71. 	Anžel A, Heider D, Hattab G (2023) Interactive polar diagrams for model comparison. Computer Methods and Programs in Biomedicine 242:107843. https://doi.org/10.1016/j.cmpb.2023.107843

72. 	Uppalapati S, Paramasivam P, Kilari N, et al (2025) Precision biochar yield forecasting employing random forest and XGBoost with Taylor diagram visualization. Sci Rep 15:7105. https://doi.org/10.1038/s41598-025-91450-w